## Slide 1: NO Oxidation on Pt/Al2O3: Kinetics study1 Prepared by: Niamul Hassan #ID 116455129 Chemical and Molecular Engineering Stony Brook University

## Slide 2
NOx mainly consists of NO and smaller amount of NO2
At high temperature inside internal combustion (IC) engine, NOx forms from N2 and O2 of air above 1500℃
  It increases with temperature.
N2 containing fuel additives also produce NOx during combustion.
Background
NOx
Courtesy: Fossil consulting services
Courtesy: Shutterstock.
Notes: NOx is shorthand for nitric oxide (NO) and nitrogen dioxide (NO2)
produced from the reaction between nitrogen and oxygen during combustion of fuels, such as hydrocarbons, in air; especially at high temperatures, such as in car engines

## Slide 3
Health concerns
Respiratory exposure causes asthma.
Exacerbates Non-respiratory diseases.
Forms ozone that damages lungs tissue
Environmental concerns
Greenhouse effect
EPA imposes regulations on NOx emission from IC engines.
  Study of NOx abatement is important.
Background
Figure: National emissions of NOx from various sources2.

## Slide 4: Experimental: Synthesis
Catalyst: 0.3wt% Pt/Al2O3
Fresh catalyst: As-synthesized, 42% Pt dispersion
Sintered catalyst: calcined at 600C for 6h in dry air
  It lowers the Pt dispersion.
  Agglomeration.

## Slide 5: Experimental: Reaction set-up
Stainless-steel packed-bed reactor.
Catalyst was wrapped in insulation to minimize bypassing of gas.
The reactor was installed into a furnace with a thermocouple.
Inlet gas was pre-heated by a separate heating furnace.
  Figure: A packed-bed reactor (PBR).

## Slide 6: Experimental: Kinetics Measurement
NO conversion < 15% to operate as differential reactor.
Data was collected after 1 hr. to ensure steady state.
Sintered sample
  To check reaction order, the concentrations of NO, O2 , and NO2 were changed 80-480 ppm, 10-25%, and 100-240 ppm one-at-a-time, respectively.
Fresh sample
  Like sintered one, reaction order was checked.

## Slide 7: Experimental: Kinetics Measurement
  Figure: Experimental data for fresh Pt/Al2O3 sample.
Notes: There are lots of data, however, we do not need all of them.

## Slide 8
Experimental: Kinetics Measurement
  Figure: Experimental data for sintered Pt/Al2O3 sample.
Notes: With this data set, first easiest thing that we can calculate is the conversion of NO.

## Slide 9
Experimental data were imported from two CSV files (fresh and sintered) using pd.read_csv.
A CSV file is easier to handle in python.
Application of Python: Importing CSV files
Notes: For that purpose, experimental dataset were imported from two CSV files using panda.read_csv.

## Slide 10
Application of Python: Activity plot
Conversion, X =
Temperature vs. Conversion
How a catalysts performs in a certain reactive condition.
Defined a function named ‘conversion’
  Depends on inlet and outlet concentration of reactant.
To get a smooth activity plot, using ‘from scipy.interpolate import make_interp_spline’ a smooth curve was fitted that passes through all sorted data points.
Notes: Defined a function named ‘Conversion’ that takes inlet and outlet concentration as input.
I expressed the conversion as percentage.
Smooth_curve fcn: This function takes two sets of data points (T and X) and creates a smooth curve between points.
make_interp_spline: fitting a smooth curve that passes through all the sorted data points.

## Slide 11
What is Arrhenius Plot?
    ln(k) vs
A straight line whose slope is the same as activation energy.
Minimum potential energy to form product(s).
1/T and ln(k) were converted to numpy from pandas.
A linear regression model was fitted to estimate R2 value and activation energy.
Slopes were determined using coef_[0].
Application of Python: Arrhenius plot
Fresh
Sintered
Notes: To get Arrhenius plot and estimate activation energy, we need to use data points where gas composition is constant, but temperature is changing, and conversion is less than 10%.
For fresh sample, 4 data points are available for Arrhenius plot.
For sintered sample, also 4 data points are available for Arrhenius plot.
1/T, ln(k) were converted to numpy arrays from pandas series.

## Slide 12
Arrhenius Plots of Both fresh and sintered samples.
Application of Python: Arrhenius plot
Notes: Ea of sintered sample is higher than the fresh one.
It was the expected outcome, because when fresh sample was heated at 600C for 6h, its morphology is changed.
Crystalline size goes up, agglomeration occurs, surface area decreases which reduces the activity.

## Slide 13
  Rate = k. [NO]n
  ln(Rate) = ln(k) + n.ln([NO])
  So, n is the slope of ln(rate) vs. ln([NO]) straight line.
  Therefore,
  reaction order, n =
Application of Python: Reaction order
Reaction order of NO for fresh and sintered samples.
Notes: 1. first, [NO] and rxn rate were extracted from CSV files.
2. Their natural log was calculated using np.log and converted into numpy arrays from pandas series.
3. Slope was estimated using np.gradient

## Slide 14
Concentration and corresponding reaction rate were imported from CSV.
Natural logarithm were calculated using np.log
Pandas series were converted into numpy array.
Estimation or rxn order using np.gradient
Output:
Application of Python: Reaction order
Reaction order of NO for fresh and sintered samples.

## Slide 15
  Rate = k. [O2]n
  ln(Rate) = ln(k) + n.ln([O2])
  So, n is the slope of ln(rate) vs. ln([O2]) straight line.
  Therefore,
  reaction order, n =
Output:
Application of Python: Reaction order
Reaction order of O2 for fresh and sintered samples.

## Slide 16
  Rate = k. [NO2]n
  ln(Rate) = ln(k) + n.ln([NO2])
  So, n is the slope of ln(rate) vs. ln([NO2]) straight line.
  Therefore,
  reaction order, n =
Output:
Application of Python: Reaction order
Reaction order of NO2 for fresh and sintered samples.

## Slide 17: References
S.S. Mulla et al. / Journal of Catalysis 241 (2006) 389–399
U.S. Environmental Protection Agency (.gov) https://cfpub.epa.gov › roe